## Dec

## Dent

…a brilliant smile!

# Bonding Instructions for Tooth Jewelry

Please note that proper attachment of the tooth jewelry is only guaranteed if you follow these recommendations.

Use a light cured, transparent, flowable composite for application.

- Disinfect the jewel in alcohol prior to the application. Do not touch the jewel with your fingers once it’s removed from the case. To guarantee maximum adhesiveness, it is essential to avoid skin contact of the coating on the backside of the jewel.

- Clean the surface of the tooth with a fluoride-free polishing paste. Completely dry and isolate the tooth.

- Apply Etchant to the enamel for about 30 sec.

- Rinse surface thoroughly with water and blow dry for 10 sec. No Etchant should remain on the tooth! Please follow protective measures.

- Apply a light-curing bonding agent. Leave it on for a max. of 10 seconds, distribute bonding through air blowing, then light-cure for 20 seconds.

Apply a small amount of flow composite to the surface of the tooth. Use a jewel handler (or a plugger with a tiny bit of Vaseline on the tip) to pick up the jewel. Press it into the center of the composite. The composite must ooze out a bit on the sides so the jewel is encircled by the Composite for macromechanical retention, but make sure the jewel is in contact with the enamel.   See picture 

- Now you may adjust the jewel while letting the patient check the desired positioning in the mirror.

- Take the light-curing lamp and start hardening the composite from the top for about 60 seconds. Light cure from the sides for a few seconds and also harden the composite from the back of the tooth for another 60 seconds making sure the composite hardens evenly. Total curing time is approximately 180 seconds. Follow instructions of the bonding-system you are using!

- You may carefully polish any sharp edges of the composite with a rubber point if needed.

Do NOT use Tweezers for handling the jewel. The sharp edges might damage the special coating on the backside of the tooth jewel.

If you have any further questions we will be happy to hear from you!